Supplementary Table S1. Full Shockley–Queisser current-limit audit of the unconstrained model short-circuit current density, Jsc,raw, against the bandgap-dependent ideal above-bandgap photon-current limit, JSQ, for 18 representative combinations of Ga fraction x, diffusion length L, and absorber thickness d. The audit spans x = 0.00 and 1.00, L = 0.3, 1.5, and 3.0 µm, and d = 0.5, 1.5, and 3.0 µm. All Jsc,raw/JSQ ratios remain below unity; no artificial post-processing current cap was applied.

| x | L (µm) | d (µm) | Jsc,raw (mA/cm2) | JSQ (mA/cm2) | Jsc,raw/JSQ | Flag |
| --- | --- | --- | --- | --- | --- | --- |
| 0.00 | 0.30 | 0.50 | 33.29 | 47.26 | 0.704 | ok |
| 0.00 | 0.30 | 1.50 | 35.27 | 47.26 | 0.746 | ok |
| 0.00 | 0.30 | 3.00 | 35.36 | 47.26 | 0.748 | ok |
| 0.00 | 1.50 | 0.50 | 33.71 | 47.26 | 0.713 | ok |
| 0.00 | 1.50 | 1.50 | 37.79 | 47.26 | 0.799 | ok |
| 0.00 | 1.50 | 3.00 | 38.52 | 47.26 | 0.815 | ok |
| 0.00 | 3.00 | 0.50 | 33.73 | 47.26 | 0.714 | ok |
| 0.00 | 3.00 | 1.50 | 38.00 | 47.26 | 0.804 | ok |
| 0.00 | 3.00 | 3.00 | 39.05 | 47.26 | 0.826 | ok |
| 1.00 | 0.30 | 0.50 | 16.49 | 24.17 | 0.682 | ok |
| 1.00 | 0.30 | 1.50 | 17.49 | 24.17 | 0.724 | ok |
| 1.00 | 0.30 | 3.00 | 17.57 | 24.17 | 0.727 | ok |
| 1.00 | 1.50 | 0.50 | 16.69 | 24.17 | 0.691 | ok |
| 1.00 | 1.50 | 1.50 | 18.75 | 24.17 | 0.776 | ok |
| 1.00 | 1.50 | 3.00 | 19.21 | 24.17 | 0.795 | ok |
| 1.00 | 3.00 | 0.50 | 16.70 | 24.17 | 0.691 | ok |
| 1.00 | 3.00 | 1.50 | 18.86 | 24.17 | 0.780 | ok |
| 1.00 | 3.00 | 3.00 | 19.50 | 24.17 | 0.807 | ok |

Note: The maximum ratio is 0.826 at x = 0.00, L = 3.0 µm, d = 3.0 µm; all 18 audited cases remain below the ideal current limit.